SOLVED EXAMPLES: MILLER INDICES

Q) Determine the Miller indices of a plane that makes intercepts of 4Å, 3Å and 8Å on the coordinate axes of an orthorhombic lattice with the ratio of the axial lengths as:

a : b : c = 2 : 3 : 1

A) This problem is about the very basic definition of Miller indices and how to derive them.

|  | X | Y | Z |
| --- | --- | --- | --- |
| Intercepts | 4Ǻ | 3Ǻ | 8Ǻ |
| Lattice parameters | 2x | 3x | 1x |
| Ratio |  |  |  |
| Reciprocal |  | x |  |
| Factoring common factors |  | 1 |  |
| Integer form | ( 4 | 8 | 1) |

Q) What are the miller indices of the line of intersection of a  and  plane in a cubic crystal?

# A) We shall arrive at the solution by a geometrical method and by an analytical method.

# Geometrical Method

# Note: ,

# Analytical Method-1

Weiss zone law states that if a direction [u v w] is contained in plane (h k l) then:

# Let [u v w] be the intersection of  and

( the indices of the direction are of the form .

As miller indices are written after factoring out common factors the miller indices are:  or the opposite direction  .

# Analytical Method-2

Using equation of a line in intercept form (a, b, c are intercepts along x, y, z axis respectively):

. Substituting the intercepts for the two planes and solving simultaneously we get the equation for the line of intersection:

(  (slope = (1 and intercept = (1)