Calculate the surface enthalpy of Cu crystal, when the external surface is of {100}, (110}, {111} type.

Bond energy of Cu (BCu) = 56.4 KJ / mole of bonds.  aCu = 3.61 Å. Use the broken bond model. Ignore surface relaxations and reconstructions.

A) The bond energy of is given for a mole of bonds. We need to convert this to bond energy per bond.

Bond E of Cu / bond (Bb) = bond energy per bond/Avogadro number = BCu / N0	= = B1 (let the bond energy per bond be equal to B1).

The multiplier half in the above equation is because two surfaces are created in one cut.

. The usual symbol for surface energy is ( (= S):   [J / m2].

Figure below shows the coordination polyhedron for FCC ( Cubeoctahedron

(100)

Area of (100) = a2. Number of atoms in this area = 2. Number of bonds broken per atom: 4.

S(100) = B1 (   (  4 (   = 2.87 J / m2

(110)

Area of (110) = A(110) =  = .

Area of the plane within the unit cell = . Number of atoms in this area: 2.

Number of bonds broken per atom: 5.

S(110) = B1 (   (  5 (   = 2.54 J / m2

(111)

Area of (111) = A(111) = = .

Number of atoms in this area: 2. Number of bonds broken per atom: 3.

In the Figure below the B (in the plane of the cut = surface plane) and C (below plane) layer bonds are intact but A layer bonds are broken (= 3 Nos).

S(111) = B1 (  (  3 (   = 2.489 J / m2