Consider the pattern below with White, Grey and Dark grey circles

(skip the concepts which you are not familiar with)

Fig.1

Let us do the following:

- Draw the conventional UC (name the UC and calculate the number of lattice points per cell).

- Draw alternate non-primitive cells.

- Identify the lattice points and the motif (name the Bravais lattice).

- Draw the fundamental (shortest) lattice translation vector and write its Miller Indices.

- Overlay symmetry operators on the figure.

- Draw some non-primitive unit cells.

- Identify the space group (Hermann-Mauguin symbol) and the Asymmetric Unit

- How to place the entities (filled and open circles) using Wyckoff labels/positions.

( Various entities are overlaid on the pattern (the solutions are shown but some thinking is required to ensure that things are in place and right!)

Fig.2

Key: m ( mirror, g ( glide (reflection), n ( diagonal glide

Notes:

The central white circle in UC1 is NOT a lattice point if the corners are chosen to be lattice points (Why?)

Though UC1 and UC2 have the same size UC1 is the conventional choice due to its higher symmetry (which is commensurate with that of the lattice- e.g. both have a 4-fold)

The motif contains: 2 while circles, 3 dark grey circles and 3 light grey circles 
(Can you ensure that this motif repeats at every lattice point?)

One of each type of entity is marked ( symmetry elements (especially translation) will overlay the complete set.

( Alternate unit cells (non-primitive)

Fig.3

Cotd…

( The UC with entities overlaid are shown below

(a)    (b)

|  | Asymmetric unit with portions/parts of the circular entities |
| --- | --- |

Fig.4

- Bravais Lattice = Primitive square lattice

- No. of lattice points per cell = 1 (UC1 or UC2 ( note that their sizes are same)

- Space group = p4gm; No. 12.

- Asymmetric Unit: x([0, 0.5],  y([0, 0.5], y ( (0.5 ( x)

Notes:

- Asymmetric unit is a tile (region of space), which along with the space group tiles space (2D here). Hence, truly speaking asymmetric unit does not contain any entities.

- In the figure above (Fig.4b), the asymmetric unit is shown overlaid with the entities (parts of circles- filled and open).

Cotd…

( Now we place the circles using Wyckoff labels/positions

|  | Wyckoff position | Coordinates | Site Symmetry | x | y | Occupancy |
| --- | --- | --- | --- | --- | --- | --- |
| A (Unfilled circle) | 2a | (0, 0), (½, ½) | 4.. | - | - | 1 |
| B (light grey circle) | 4c | (x, x + ½), ((x, (x + ½) ((x + ½, x) (x + ½, (x) | ..m | 0.35 | - |  |
| C (dark Grey circle) | 4c | (x, x + ½), ((x, (x + ½) ((x + ½, x) (x + ½, (x) | ..m | 0.15 |  |  |

Notes:

When points are plotted according to the coordinates given in the table (for say 4c grey circle); some of the points are in the negative x or y axis. Unit values are added to these appropriately to bring them back into the unit cell.

Replot →

Please also refer to: from_L+M_SG.ppt