## Slide 1: Dielectric Materials
Topics to discuss
  Principles of dielectrics
  Dielectrics Loss and Breakdown
  Polarizations
  Frequency dependence
  Ferro-, Piezo- and Pyro- electrics
ESO 205
Nature and Properties of Materials

## Slide 2: Why are these important?
A variety of applications
  Sensors
    Force, strain and temperature sensing
  Actuators
    Example: quartz watches, piezoelectric motor
  Memories or data storage
    DRAMs, FRAMs
  Transducers
    Naval and aerospace applications

## Slide 3
http://www.eetimes.com/document.asp?doc_id=1276895
DRAMs
Materials:
SiO2, Ta2O5, HfO2

## Slide 4
High-force high-deflection piezoelectric diaphragm actuator
Materials:
Pb(ZrTi)O3, BaTiO3, PbTiO3

## Slide 5
http://www.wtec.org/loyola/mems/c5_s3.htm
Yokogawa resonant pressure sensor
The resonator is excited by the application of an alternating current in a DC magnetic biasing field, with a variable-gain amplifier used to maintain a constant vibration amplitude.

## Slide 6: Basic Characteristics
At zero field, the centers of positive and negative charges coincide.
Upon application of a dc or static electric field, there is short range migration of charges.
However, there is a limited movement of charges leading to the formation of charge dipoles and the material, in this state, is considered as ‘polarized’. These dipoles are aligned in the direction of the applied field.
E

## Slide 7: Basic Characteristics
The applied field can also align the dipoles that were already present in the material i.e. material containing dipoles without application of the field.
  Polar materials
Of course, both these effects may be present in single material i.e. dipoles can be aligned as well as be induced by the applied field.
Net effect is called as ‘Polarization’ of the material.

## Slide 8
Dipole Moment (C.m)
Polarization (C/m2)
(Dipole moment per unit volume)
So, if all the dipoles were aligned in a direction, then
P=N.
Conversely, if all the dipoles were aligned in random directions, then
P=N.Σ=0
Vectors

## Slide 9: Capacitor
The air-gap can store energy
If we can move charges temporarily, more charge can be stored
Bound charge around ionic cores in a material can lead to dielectric properties
Dipolar Polarization
Surface charge
Not possible to distinguish between two by Gauss’s law

## Slide 10: Polarization and Surface Charge
Surface charge density

## Slide 11: Parallel Plate Capacitor (Vacuum)
Maxwell Equation

## Slide 12: Capacitor with a Dielectric
εr : Relative dielectric constant of the dielectric (>1)
As a result to sustain same polarization, the voltage dropped reduces.
In other words, other requires lesser voltage to sustain similar charge storage OR
If the voltage is kept same, the charge density goes up.
This is what works for DRAMs with high dielectric constant materials.

## Slide 13: Capacitor with a Dielectric

## Slide 14
For a capacitor in vacuum
For a capacitor with a dielectric
Extra term due to Dielectric
Dielectric Displacement

## Slide 15
Dielectric susceptibility
Susceptibility is ratio of polarized charge or excess charge to the surface charge in a vacuum capacitor: expresses response of the capacitor to the applied field, determined by dielectric constant.

## Slide 16
air | 1.005364
glass | 4 - 7
glass, pyrex 7740 | 5.0
gutta percha | 2.6
jet fuel (jet a) | 1.7
lead oxide | 25.9
lead magnesium niobate | 10,000
lead sulfide (galena) | 200
lead titanate | 200
paper | 3.3, 3.5
plexiglas | 3.1
polyester | 3.2 - 4.3
polyethylene | 2.26
polypropylene | 2.2 - 2.3
polystyrene | 2.55
polyvinyl chloride (pvc) | 4.5
porcelain | 6 - 8
potassium niobate | 700
potassium tantalate niobate, 0 ℃ | 34,000
potassium tantalate niobate, 20 ℃ | 6,000
diamond | 5.87
quartz, crystalline | 4.60
quartz, fused | 3.8
rubber, vulcanized | 2.9
salt | 5.9
selenium | 6.0
silicon | 11.8
silicon carbide (αSiC) | 10.2
silicon dioxide | 4.5
silicone oil | 2.7 - 2.8
soil | 10 - 20
strontium titanate, +25 ℃ | 332
strontium titanate, –195 ℃ | 2080
sulfur | 3.7
tantalum pentoxide | 27
teflon | 2.1
tin antimonide | 147
tin telluride | 1770
titanium dioxide (rutile) | 114

## Slide 17
Ref: Materials Science and Engineering, Callister

## Slide 18: Compare Optical (index of refraction) and Electrical Measurements of 
εr = n2
Electromagnetic Theory
Electronic Polarization
Electronic and Ionic Polarization
Electronic, Ionic and Dipolar Polarization

## Slide 19: Origin of Polarization
True dipoles creating polarization in materials (not surface effect)
What is the response of these various dipole mechanisms to various E-field frequencies?
Polarization mechanisms and their frequency dependence
  electronic polarization
  ionic polarization
  molecular polarization

## Slide 20: Types of Polarization
Electronic Polarization (e)
Elemental solids
Ionic solids
Ionic Polarization (i)

## Slide 21
Orientation Polarization (o)
Polar Molecules such as Ice

## Slide 22
Interfacial Polarization (o)

## Slide 23: Frequency Dependence
Increasing Mass of dipole

## Slide 24: Dielectric Constant vs. Frequency
Space Charge
Ionic
Dipolar
Electronic

## Slide 25
Material | r | n2 | Dominant mechanisms
C (Diamond) | ~5.7 | 5.85 | Electronic
Ge | ~16 | 16.73 | Electronic
NaCl | ~5.9 | 2.37 | Electronic and Ionic
Water (H2O) | ~80 | 1.77 | Electronic, Ionic and Dipolar

## Slide 26: Dielectric Strength
Intrinsic Mechanisms
  Rise in electron temperature
  Population increase in the conduction band
Thermal Breakdown
  Joule heating, faster than dissipation
  Reduces the intrinsic dielectric strength
Discharge breakdown
  Ionization in the vicinity of the dielectric followed by subsequent breakdown
1: Free ions accelerated by the field induce a current.
2: These will be saturated after a certain voltage and give a constant current,
3 and 4: Caused by ion avalanche
Parameter of usefulness
Defined as maximum field which dielectric can withstand before failure
Marked by sudden and rapid increase in the conductivity i.e. high electron concentration in the conduction band.

## Slide 27: Classification of Dielectrics
Non-polar dielectrics
  Dielectrics having no dipole moment in the absence of electric field
  Example: Inert gases, N2, CH4
Polar Dielectrics
  Dielectrics having finite dipole moment in the absence of electric field
  Permanent dipole moment
  Example; H2O, CH3Cl etc
+
-
+

## Slide 28: Crystallographic Considerations
Total of Crystal systems: 7
Bravais Lattices: 14
Point groups: 32 (based on symmetry considerations)

## Slide 29: Center of Symmetry
The term centrosymmetric refers to a space group which contains an inversion center as one of its symmetry elements
For every point (x, y, z) in the unit cell, there is an indistinguishable point (-x, -y, -z).

## Slide 30
Crystal class
Cubic
Tetragonal
Orthorhombic
Hexagonal
Trigonal
Monoclinic
Triclinic
Total Number
Noncentrosymmetric Point groups |  |  |  |  | 
Polar |  | Non-polar |  |  | 
none |  | 432 |  | 3m | 23
4 | 4mm | 4 |  | 42m | 22
mm2 |  | 222 |  |  | 
6 | 6mm | 6 | 6m2 | 622 | 
3 | 3m | 32 |  |  | 
2 | m | none |  |  | 
1 |  | none |  |  | 
10 groups |  | 11 groups |  |  | 
Centro symmetric Point groups | 
m3 | m3m
4 or m | 4 or mmm
mmm | 
6 or m | 6 or mmm
3 | 3m
2 or m | 
1 | 
11 groups | 

## Slide 31
Noncentrosymmetric Point groups |  |  |  |  | 
Polar |  | Non-polar |  |  | 
none |  | 432 |  | 3m | 23
4 | 4mm | 4 |  | 42m | 22
mm2 |  | 222 |  |  | 
6 | 6mm | 6 | 6m2 | 622 | 
3 | 3m | 32 |  |  | 
2 | m | none |  |  | 
1 |  | none |  |  | 
10 groups |  | 11 groups |  |  | 
Piezoelectrics
(except 432)
X
F

## Slide 32
Noncentrosymmetric Point groups |  |  |  |  | 
Polar |  | Non-polar (X) |  |  | 
none |  | 432 |  | 3m | 23
4 | 4mm | 4 |  | 42m | 22
mm2 |  | 222 |  |  | 
6 | 6mm | 6 | 6m2 | 622 | 
3 | 3m | 32 |  |  | 
2 | m | none |  |  | 
1 |  | none |  |  | 
10 groups |  | 11 groups |  |  | 
Pyroelectrics
X
(10 Polar Groups)

## Slide 33: Pyroelectrics
Polar Crystals
  These crystals can be spontaneously polarized and polarization can be compensated through external or internal conductivity or twinning or domain formation.
Since spontaneous polarization depends upon the temperature, a change is temperature leads to development of electric charge on faces of the crystal perpendicular to the polar axis.
  Pyroelectric effect.
  All 10 classes of polar crystals are pyroelectric.

## Slide 34: Ferroelectrics
In the some of these polar non-centrosymmetric crystals, the polarization along the polar axis can be reversed by reversing the polarity of electric field.
  Ferroelectric materials
  Spontaneously polarizable with reversible polarization.

## Slide 35
20 Noncentrosymmetric PGs
10 polar PGs

## Slide 36
Piezoelectric Materials: Non Centro-symmetric structure is only requirement
Applications: Transducers, Resonators etc.
Stress
Charge development
Piezoelectric Effect

## Slide 37: Piezoelectric effect

## Slide 39: Applications
Actuators
Atomic force microscopes and scanning tunneling microscopes
Inkjet printers
Diesel engines
X-ray shutters
XY stages for micro scanning used in infrared cameras.
Motion of a patient precisely inside active CT and MRI scanners
Ultrasound imaging
Buzzer

## Slide 40: Piezoelectric effect
Unit Cell at Rest
-
+
+
-
+
-
Neutral Charge
Unit Cell Under Mechanical
Compression (“pushing” force):
Electrical polarity as shown
-
+
+
-
+
-
Unit Cell Under mechanical
Tension (“pulling” force):
Electrical polarity reverses.
+ + +
- - -
+ + +
- - -
+
“+” = Silicon
“-” = Oxygen

## Slide 41: Piezoelectric effect
P: polarization
F: Force

## Slide 42: Piezoelectric effect
Linearity of piezo-effect

## Slide 43: Piezoelectric effect
PVDF

## Slide 44: Pyroelectricity
In addition to piezoelectricity, have a unique polar axis
Non-centrosymmetric crystals exhibit this effect
Applications: imaging, detectors
T
Charge
where p = pyroelectric coefficient (C m-2 T-1).

## Slide 45: Ferroelectricity
Pyroelectric materials with reversible polarization upon reversal of applied field
Remnant polarization at zero field
Applications
  Memories
  Sensors
  Actuators

## Slide 47: Domain Formation
Reorientation of domains in a polycrystalline ferroelectric material after poling
before poling, PR=0
After Poling, PR0
E
PR

## Slide 48: Dielectric Const vs Temperature
Vaiation of Dielectric constant and polarization with temperature (Potassium Dihydrogen Phosphate, a ferroelectric)

## Slide 49
Spontaneous Polarization: Ferroelectrics
The Curie-Weiss law illustrated for (Ba,Sr)TiO3
From L.L.Hench and J.K.West,Principles of Electronic Ceramics,Wiley,1990,p.243.
Curie-Weiss Law

## Slide 50: Ferroelectrics
Each unit cell a dipole!
Large PR (remnant polarization, P(E=0))
Coercive Field EC, electric field required to bring P back to zero.

## Slide 51: Ferroelectrics
A
B
(a)
(b)
Schematic representation of structure and dipoles in a hypothetical 2-D crystal
A
O
B
A typical ABO3 perovskite unit-cell e.g. PbTiO3. Remanent polarization is zero when the structure is cubic (paraelectric phase) and it is non-zero in the ferroelectric phase which has tetragonal structure.
Most ferroelectrics are perovskite structured
Lack of a centre of symmetry is a requirement: most ferroelectric materials are Tetragonal or orthorhombic
Local metastable positions away from equilibrium are created

## Slide 52: Properties of Common Ferroelectrics

## Slide 53: Perovskite Structure
ABO3 type of structure: BaTiO3 , CaTiO3 , SrTiO3,
Distortions common: could be non-cubic
Known as the BaTiO3 or CaTiO3 lattice
Three different atoms in the base: ABO3
A at (0,0,0), O at (½, ½, ,0) and B at (½, ½, ½).
  Primitive Cubic Lattice
Co-ordinations
  B: Octahedral
  A: 12-fold

## Slide 54: Perovskite

## Slide 55: Tetragonal BaTiO3

## Slide 56: Tolerance Factor
t=1 for ideal perovskite
t<1 for most perovskite with distorted structures

## Slide 57
Dimensions of a pseudocubic unit-cell of BaTiO3 (Phil Mag, 7, 1019, (1949))
Temperature dependence of dielectric constant (Phys. Rev., 76, 1221 (1949)

## Slide 58: Summary
Dielectrics are insulating materials with Eg > 3 eV
A dielectric material increases the charge storage capacity of plate capacitor: dielectric constant
Every dielectric has a breakdown strength
Types of polarization
  Electronic, Ionic, Molecular, Space charge
  Strong frequency dependence
Dielectrics can be defined as Polar and Nonpolar dielectrics
Polar dielectrics are those having finite dipole moment at RT
  Defined as Ferro-, Pyro- and Piezo-electrics depending on the nature of polarization and dependence on stress, temperature and electrical field.
  Find applications in variety of areas